PRAMOLIT S22

Описание

Пропитывающее средство, активные компоненты которого проникают в материалы с низкой пористостью за счет входящих в состав специальных растворителей.

Возможно использовать только на поверхностях, устойчивых к входящим в состав средства растворителям. Активные компоненты также повышает гидрофобные и олеофобные свойства обработанной поверхности, не закупоривая при этом поры.

Область применения

Для поверхностей из необработанной плитки, плитки с силиконовым слоем, малоабсорбирующего натурального камня, гранита, керамической черепицы и кирпича.

Для половых поверхностей в кухонной зоне.

Дозировка

Применяется в концентрированном виде.

Инструкция по применению

Нанесите в концентрированном виде на предварительно обезжиренную, промытую и хорошо высушенную поверхность пола и равномерно распределите полировочной машиной, кистью или валиком. Дайтепропитке высохнуть. Повторное применение возможно через 3 -5 часов. Полное высыхание достигается через 24 часа.

Расход продукта

Первая пропитка: 60 - 100 г на 1 м2 в зависимости от впитывающей способности обрабатываемой поверхности.

Последующие пропитки: 30 - 50 г на 1 м2.

Совет

Для ежедневного использования можно использовать средство совместно с очень слабым раствором моющего средства (например, с чистящим средством на основе спирта)

Если необходимо, повторите процедуру через один год.

Производитель не несет ответственности за повреждения в случае неправильного использования продукта.

Технические характеристики

Стойкость при хранении:		2 года.

Хранение:				никаких особых требований.

Состав:	Пропитывающие вещества, углеводороды.

# pramolit S-22

General

The product is based on impregnating agents in special solvents which help penetrating the active ingredients in low porosity materials such as granite.

It should only be used on solvent-resistant surfaces.

Special water-repellent and oil-repellent ingredients effectively hinder oil and grease splashes and spoilt drinks from penetrating into absorbent terracotta tiles, clicker bricks and natural stone slabs.

Does not close the pores, which hinders film establishment. The floor’s appearance remains natural.

Colours do practically not darken.

Suitable for untreated tiles and tiles with a silicone layer.

Application areas

Especially suitableforlessabsorbentnatural stone, clay tilesandbricks.

Is suitable for the high requirements in kitchens.

Dosage

Use sparingly and undiluted.

Instructions for use

Vacuum or wipe floor.

Clean heavily soiled floors with water and allow to dry.

Clean old or stained floors with a solvent cleaner before.

Apply product undiluted to the clean, dry surface with a paint brush, roller or polish applicator. Do not apply more than the floor is able to absorb.

Allow to dry.

The floor can be used again after 3 - 5 hours.

Full impregnation effect after 24 hours.

Product consumption

First impregnation:		approx. 60 - 100 g/m², depending on absorbency

Follow-up impregnation:	approx. 30 - 50 g/m2

Special advice

Do not impregnate as long as any salt blistering/blooming are visible.

If any application tracks are visible, too much material was used. Wipe with a clean, dry cloth to remove them.

For daily care, impregnated floors can be maintained with a very diluted detergent solution (e.g. alcohol cleaner.)

If necessary, repeat impregnation after one year.

The manufacturer declines all responsibility for damages from improper product use.

Technical data

Storage stability:	at least 2 years

Storage:	store in original packaging

Ingredients:	impregnation components, hydrocarbons.